Kohltech International Architectural Details

Select Double Hung

System Features	2

Structural Performance	4

Thermal Performance	5

Section Details: Select Double Hung Head/Sill, Jamb Details	8

Section Details: Fixed Head/Sill, Jamb Details	10

Section Details: Mullion Details	11

Section Details: Exterior Options	13

NOTE:

Specifications and technical data are subject to change without notice.

Allow 1/16” (2mm) tolerance on all measurements.

Metric measurements are shown in parenthesis.

For accessories dimensions and applications see the Accessories section of this manual.

For technical assistance you may call 1-800-565-4396 or visit our website:

www.peterkohler.com

# System Features

Frame:

- Standard is white extruded polyvinyl chloride (uPVC) profiles.  Optional tan extruded.

- Operator/Fixed Frame depth: 3.25” (83mm)

- Small Picture Window Frame depth: 3.25” (83mm).  This profile is used for shapes.

Sash:

- Standard is white extruded polyvinyl chloride (uPVC) profiles.  Optional tan extruded.

Interior and exterior finish

- Interior finish: Standard high gloss white.  Optional tan.

- Exterior finish: Standard high gloss white.  Optional tan

- Additional colours are also available: waterborne single component color coating system which is chemically bonded to the exterior vinyl surface.

Hardware

- Truth lock and keeper

- John Evans constant force balance

- Stainless pivot bars

Weather Stripping:

- Two pile weather strip on sash

Jamb Extensions:

- Jamb extensions available for various depths and factory applied.

Insect Screens:

- White aluminum full screen standard. Optional tan to match tan extruded frame and sash.

- Screen mesh: grey fiberglass standard.

- Pull tabs integrated into screen corner

Interior / Exterior Simulated Divided Lites (SDL):

- Interior bar: Extruded vinyl or wood, 3/4” and 1” wide bars.  Standard white.  Optional tan or painted.

- Exterior bar: Extruded vinyl, 3/4” and 1” wide bars.  Standard white.  Optional tan or painted.

- Pattern: Rectangular, custom lite layouts available, contact your Kohltech International representative

Between the Glass Grilles:

- 3/4” Contoured Georgian.  Standard white.  Optional tan, painted any standard color, or spilt finish interior/exterior.

- 1” Contoured Georgian.  Standard white.  Optional painted any standard color.

- 5/8” Flat Colonial.  Standard white.  Optional tan, brass, brushed aluminum, painted.

- Slimline 5/16” Flat Colonial.  Standard white.  Optional tan, pewter, black, gold, mill finish, painted.

Glazing:

- Glazing method: Insulated glass, hermetically sealed

- Glazing seal: Tape glazed, silicone heel bead

- Glazing type: Clear glass

- Spacer type: Warm edge steel Intercept

- Options: soft coat LoE, argon gas fill, obscure glass, tinted glass, Energlas (LoE/Argon and Stainless Steel spacer), Energlas Plus (triple paned, 2 panes with LoE glass, argon gas filling, and Edgetech warm edge Superspacer)

Accessories:

- Standard: ½” to ¾” return is built into the frame on the interior.

- Optional:  7/8”,1½”; 2”, or 3 ½” brick molding all four sides or with subsill.  All available with J-trim and nailing fin.  2” and 3 ½” brick molds available with decorative backband molding.

- Installation brackets

# Structural Performance

| Select Double Hung Performance Data – CSA A440 |
| --- |
|  | Gateway Size | Air Resistance | Water Resistance | Wind Load Resistance |
| Select Double Hung | 39” x 63” 40" x 63" | N/A A2 | N/A B3 | N/A C3 |
| Select Double Hung Picture | 74-7/8 x 74-7/8 50 x 100 72 x 80 | FX FX FX | B7 B7 B7 | C4 C3 C4 |

| Select Double Hung Series Performance Data - NAFS |
| --- |
|  | Gateway Size | Rating | Canadian Air Infiltration |
| Select Double Hung | 39 x 63 40 x 63 | N/A R-PG50-H | A2 A2 |
| Select Double Hung Picture | 74-7/8 x 74-7/8 50 x 100 72 x 80 | N/A R-PG40-FW LC-PG55-FW | N/A FX FX |

| NAFS (AAMA/CSA-A440) Performance Grade Indicators |
| --- |
| Product Performance Classes | Minimum Performance Grade | Minimum Design Pressure | Minimum Structural Test Pressure | Minimum Water Penetration Test Pressure |
|  | PG | psf | (Pa) | psf | (Pa) | psf | (Pa) |
| R – Residential | 15 | 15 | (719) | 2.90 | (137) | 2.90 | (137) |
| LC – Light Commercial | 25 | 25 | (1198) | 3.75 | (180) | 3.75 | (180) |
| CW – Commercial | 30 | 30 | (1437) | 4.50 | (217) | 4.50 | (217) |
| AW – Architectural | 40 | 40 | (1916) | 8.00 | (383) | 8.00 | (383) |

# Thermal Performance

| Select Double Hung Average Unit Thermal Performance Data |
| --- |
|  | U-value Btu/h•ft.2•°F (W/m2•K) | R-value | SHGC | VT | ER Number | Condensation Resistance | Canadian Energy Star Zone | US Energy Star |
| Select Double Hung |
| Clear | 2.7(0.48) | 2.08 | 0.59 | 0.63 | 12 |  |  |  |
| LoE | 2.0(0.36) | 2.78 | 0.54 | 0.62 | 25 | 51 |  |  |
| LoE/Argon | 1.8(0.32) | 3.13 | 0.54 | 0.62 | 30 | 54 | ABC | ER |
| Energlas | 1.8(0.31) | 3.23 | 0.54 | 0.62 | 31 | 57 | ABC | ER |
| Energlas-S | 1.8(0.31) | 3.23 | 0.54 | 0.62 | 31 | 57 | ABC | ER |
| LoE-LSG | 1.9(0.34) | 2.94 | 0.30 | 0.54 | 13 | 52 |  |  |
| LoE/Argon-LSG | 1.8(0.31) | 3.22 | 0.30 | 0.54 | 17 | 56 | A | U |
| Energlas-LSG | 1.6(0.29) | 3.45 | 0.30 | 0.54 | 20 | 58 | A | U |
| Energlas-S-LSG | 1.6(0.29) | 3.45 | 0.30 | 0.54 | 20 | 59 | A | U |

| Select Double Hung Average Unit Thermal Performance Data |
| --- |
|  | U-value Btu/h•ft.2•°F (W/m2•K) | R-value | SHGC | VT | ER Number | Condensation Resistance | Canadian Energy Star Zone | US Energy Star |
| Select Double Hung Picture Window |
| Clear | 2.7(0.47) | 2.13 | 0.64 | 0.68 | 18 |  |  |  |
| LoE | 1.9(0.34) | 2.94 | 0.59 | 0.67 | 32 | 53 | ABC | ER |
| LoE/Argon | 1.7(0.30) | 3.33 | 0.59 | 0.67 | 37 | 56 | ABCD | ER |
| Energlas | 1.7(0.30) | 3.33 | 0.59 | 0.67 | 37 | 57 | ABC | ER |
| Energlas-S | 1.6(0.29) | 3.45 | 0.59 | 0.67 | 38 | 60 | ABC | ER |
| LoE-LSG | 1.8(0.32) | 3.13 | 0.33 | 0.59 | 19 | 52 | A | U |
| LoE/Argon-LSG | 1.6(0.28) | 3.57 | 0.33 | 0.59 | 24 | 55 | AB | U |
| Energlas-LSG | 1.6(0.28) | 3.57 | 0.33 | 0.59 | 24 | 58 | A | U |
| Energlas-S-LSG | 1.5(0.27) | 3.7 | 0.33 | 0.59 | 25 | 61 | AB | U/ER |

Canadian Energy Star Climate Zones

| Energy Star Requirements for Windows (2004) |
| --- |
|  | Maximum U-values and Minimum R-Values |  | Minimum Energy Rating (ER) Values (Maximum U-value 2.00 W/m2•K) |
| Zone | U-value (W/m2•K) | U-value (Btu/h•ft.2•°F) | R-Value (ft.2•h•°F/Btu) |  | Operating Windows | Fixed Windows |
| A | 2.00 | 0.35 | 2.9 | Or | 17 | 27 |
| B | 1.80 | 0.32 | 3.2 | Or | 21 | 31 |
| C | 1.60 | 0.28 | 3.6 | Or | 25 | 35 |
| D | 1.40 | 0.25 | 4.0 | Or | 29 | 39 |

For more information please visit:

http://oee.nrcan.gc.ca/energystar/english/consumers/ratings.cfm

United States Energy Star Climate Zones

# Section Details: Select Double Hung Head/Sill, Jamb Details

# Section Details: Fixed Head/Sill, Jamb Details

# Section Details: Mullion Details

# Section Details: Exterior Options

Section Details: Interior Options